FAST-PROC-088

Revision A

FAST ANTENNA CYLINDER

FABRICATION PROCEDURE

GD1524454

Prepared by:

Ken Hersey			Date

Antenna Engineer

Approved by:

Carroll Clatterbuck	Date

Code 313.2

Approved by:

Andy Hovanec		Date

Materials Engineer

Approved by:

Giulio Rosanova		Date

Mechanical Lead Engineer

Approved by:

Jim Watzin			Date

Systems Manager

Approved by:

Ron Kolecki		Date

Flight Assurance Manager

This procedure describes the fabrication of the FAST Antenna Cylinder, GD1524454. All steps are correlated by Event Number to the certification log for this part.

Handling: At all times, the antenna cylinder should be handled with clean gloves. No ESD precautions are necessary.

A mix record should be completed and kept with the certification log for all steps involving the preparation of epoxies.

Material List

RT/Duroid 6002 substrate, 1 oz. copper clad both sides

for cylinder and strap (GD1524457)

Upper Mounting Ring (GD1524247)

Lower Mounting Ring (GD1524248)

Epon 828

Versamid 140

Silflake 135

Equipment List

Thermal Oven, capable of 177°C, with programmer

Liquid Nitrogen for cooling thermal oven

3" diameter Hose Clamps

8" diameter Aluminum mandrel

5 1/4" diameter Aluminum mandrel

5" long Aluminum block with 2.90" concave radius of curvature

5" long Aluminum block with 2.78" convex radius of curvature

Teflon sheet to wrap blocks

Small ‘C’-clamps

Metal Spatula

Metal Mircotool Chisel

Small brush for applying a thin epoxy coat

10. Receive etched, plated, and routed board and strap (GD1524457) from vendor

a. This part is covered by a separate certification log developed by the vendor, who is responsible for delivering the parts.  _____

12. Stamp Serial Number and Drawing Revision

a. Ink stamp the serial number and the latest drawing revision number, noted on the certification log, onto the board per Special Payloads Division Process No. 3, Spacecraft Part Identification Marking. _____

20. Form board into a cylinder, with 177°C 1hour soaks between operations

a. Manually form the board around an 8" diameter mandrel so that the curvature is started. _____

b. Secure the board with this large radius of curvature with standard hose clamps. _____

c. Place the board in an oven which is set to rise at 8°C/min, hold at 177°C for 1 hour, and fall at 8°C/min. The long 18" bottom edge of the cylinder should be on the oven floor. _____

d. Run the oven program. _____

e. Remove the board from the oven, and remove the hose clamps. _____

f. Repeat steps a-e until the board has reached the 4" radius of curvature. (This step may take about 2 bend treatments). _____

g. Repeat steps a-e with a smaller mandrel, 5 1/4" in diameter, until the board edges can meet, with each step making a small decrease in the board's radius of curvature. (This step may take about 3 bend treatments.) _____

30. Receive mounting rings (GD1524247-8) from vendor

a. These parts are covered by separate certification logs developed by the vendor, who is responsible for delivering the parts. These parts have already been cleaned (etched) and helicoils have been installed. _____

40. Form strap to match radius of cylinder

a. Clamp the strap between the two blocks of aluminum whose inside surfaces have been machined to form the strap to match the inside surface of the cylinder (2.90" and 2.78" radius of curvatures). Wrap the aluminum blocks with a teflon sheet to prevent marking the strap and cylinder surface. _____

50. Place cylinder into rings, heat 177°C 1hour with strap in place

a. Place the bottom end of the cylindrical board into the lower mounting ring’s board slot. _____

b. Place the top end of the cylindrical board into the upper mounting ring’s board slot. _____

c. Use one of two ‘C’-clamps to secure the strap using the two teflon sheet covered aluminum blocks to the cylinder with one block on the strap, and the

other on the outside of the cylinder. Position the clamp about 1/3 from the top of the cylinder. _____

d. Remove the lower mounting ring from the assembly. _____

e. Use the other ‘C’-clamp to also secure the aluminum blocks. Position the clamp about 1/3 from the bottom of the cylinder. _____

f. Remove the upper ‘C’-clamp from the assembly. _____

g. Remove the upper mounting ring from the assembly. _____

h. Re-clamp the aluminum blocks, positioning the upper clamp about 1/3 from the top of the cylinder. _____

i. Place the cylinder in an oven which is set to rise at 8°C/min, hold at 177°C for 1 hour, and fall at 8°C/min. The cylinder may lie on its side due to the presence of the ‘C’-clamps. _____

j. Run the oven program. _____

k. Remove the assembly from the oven and unclamp. _____

60. Epoxy strap to cylinder with Epon 828/Versamid 140 (50:50) with Silflake 135 (20:80), allow to dry clamped for 48 hours

a. Place the bottom end of the cylindrical board into the lower mounting ring’s board slot. _____

b. Place the top end of the cylindrical board into the upper mounting ring’s board slot. _____

c. Code 313.2 will provide the following conductive epoxy: _____

1. Prepare an epoxy as follows: _____

Epon 828		50 pbw

Versamid 140	50 pbw

2. Mix this epoxy as follows to form a conductive epoxy: _____

Epoxy in step a.	20 pbw

Silflake 135		80 pbw

d. With a metal spatula, apply the conductive epoxy to the convex side of the strap. _____

e. With two ‘C’-clamps, secure the strap on the inside of the cylinder centered where the board edges meet with the two polyethylene plastic covered aluminum blocks (as used in Event 40). _____

f. Allow the assembly to dry at room temperature for 48 hours before handling. _____

g. A complete cure will take 7 days at room temperature. This should be achieved before Strength Verification is performed on the antenna. _____

70. Remove excess epoxy from bond area

a. Remove the clamps, aluminum blocks, and mounting rings from the assembly. _____

b. Remove the excess conductive epoxy from around the strap bond area with a small metal microtool chisel. Care should be taken not to penetrate the ground plane and exposing the dielectric (some small scrapes which do not penetrate are considered acceptable). _____

80. Seal bond with a brush coating of Epon 828/Versamid 140 (50:50), allowing to dry for 48 hours

a. Code 313.2 will provide the following epoxy: _____

1. Prepare an epoxy as follows: _____

Epon 828		50 pbw

Versamid 140	50 pbw

b. Brush a thin coat (3-5 mils) of this epoxy on the strap bond area which will seal this area, preventing the conductive epoxy from flaking off and posing a contamination problem. _____

c. Allow the cylinder to dry at room temperature for 48 hours before handling. _____

d. A complete cure will take 7 days at room temperature. This should be achieved before Strength Verification is performed on the antenna. _____