FAST-PROC-091

FAST ANTENNA ASSEMBLY

FABRICATION PROCEDURE

GD1524452

Prepared by:

Ken Hersey			Date

Antenna Engineer

Approved by:

Carroll Clatterbuck	Date

Code 313.2

Approved by:

Andy Hovanec		Date

Materials Engineer

Approved by:

Giulio Rosanova		Date

Mechanical Lead Engineer

Approved by:

Keith Parrish		Date

Thermal Lead Engineer

Approved by:

Dave Everett		Date

Electrical Lead Engineer

Approved by:

Ron Kolecki		Date

Flight Assurance Manager

This procedure describes the fabrication of the FAST Antenna Assembly, GD1524452. All steps are correlated by Event Number to the certification log for this part.

Handling: At all times, the antenna cylinder shall be handled with clean gloves. No ESD precautions are necessary.

A mix record shall be completed and kept with the certification log for all steps involving the preparation of epoxies.

All steps that require torquing of hardware shall be witnessed by SMEX QA.

Material List

Antenna Cylinder (GD1524454)

Upper Mounting Ring (GD1524247)

Lower Mounting Ring (GD1524248)

Antenna Studs (GC1524259)

Upper Ground Plane (GD1524453)

Lower Ground Plane (GD1524459)

(6) Upper Spacers (GC1524455)

(6) Lower Spacers (GC1524456)

Jack Receptacle with Sliding Contact (2058-5305-00)

(4) #6-32 nut (MS35649-264)

(2) #4-40 bolt, 3/8" long (NAS1352N04-6)

(4) #4 belleville washer (B0250-009-S)

(2) #4 flat washer (MS15795-803)

(2) #4-40 lock nut (MS21043-04)

(12) #6-32  bolt, 3/8 " long (NAS1352N06-6)

(12) #6 flat washer (MS15795-805)

#22 bus wire

60 Sn/40 Pb solder

NS53B green paint

ITO Kapton

Y966 transfer adhesive

Stycast 2850FT

Catalyst 9

Epon 828

Versamid 140

Silflake 135

Equipment List

Torque Wrench 25 in-lbs

SMA Torque Wrench 8 in-lbs

Connector Saver (2082-5133-00)

#18 Gauge Needle for epoxy syringe

Metal Spatula

Equipment List (continued)

Torque Wrench 15 in-lbs

Torque Wrench 10 in-lbs

Hand Drill with 90° attachment

Small brush for applying a thin epoxy coat

Vector Network Analyzer with plotter

Anechoic Chamber with radiation pattern measurement equipment

Standard Gain Horn (12-1.7)

Scale capable of at least 2 lbs.

10. Mask and paint mounting rings

All painting operations during this event are per a Code 724.1 approved procedure, GSFC Procedure for the Formulation/Application of a Family of Silicate Based Electrically Conductive Thermal Control Coatings.

a. Mask the 0.070" board slot in the upper ring GC1524247. _____

b. Mask the 0.070" board slot in the lower ring GC1524248. Also, mask the six mounting holes (with the helicoils) and the 0.250" and 0.066" diameter jack receptacle holes. _____

c. Paint both mounting rings with NS53B green paint. _____

d. Allow to dry at room temperature for 24 hours. _____

20. Torque the jack receptacle into the lower mounting rings at 25 in-lbs

a. Follow M/A-COM Omni-Spectra Assembly Procedure No. 20-800 Rev. 051, steps 1,2,4, and 5, for mounting the jack receptacle, 2058-5305-00, into the lower ring. Per the procedure, a torque wrench, 2098-0248-54, calibrated to 25 in-lbs, is employed. _____     _____ (QA)

Torque Wrench ID:  _____	Cal Due: _____

30. Torque a connector saver onto the jack receptacle at 8 in-lbs

a. Hand mate a connector saver, 2082-5133-00, onto the jack receptacle. _____

b. Torque the connector saver with a torque wrench, calibrated to 8 in-lbs. _____     _____ (QA)

Torque Wrench ID:  _____	Cal Due: _____

40. Receive two antenna studs (GC1524259) from vendor

a. This part is covered by a separate certification log developed by the vendor, who is responsible for delivering the parts. _____

50. Perform fit check onto spacecraft Axial Boom

a. Place the bottom of the antenna cylinder GD1524454 edge into the lower ring’s board slot. The cylinder should be rotationally aligned such that the 0.60" x 0.22" cutout is centered around the connector block. _____

b. Place the upper ring onto the top of the antenna cylinder edge. The ring should be rotationally aligned such that two holes in each ring for the antenna studs are collinear. Placing the two antenna studs initially through the upper ring may help to obtain the alignment. _____

c. Insert both studs into the lower ring, through to the upper ring. _____

d. Place MS35649-264 nut onto each stud’s thread — do not tighten. _____

e. Install the antenna to the spacecraft per FAST-PROC-092. _____

f. Torque both antenna studs to 15 in-lbs. The axial boom mating ring at the lower mounting ring should not warp during this operation. _____     _____ (QA)

Torque Wrench ID:  _____	Cal Due: _____

g. Thread another MS35649-264 nut on the antenna studs and torque against the lower nut to 15 in-lbs. The interface to the axial boom mating rings should now be flush. _____     _____ (QA)

Torque Wrench ID:  _____	Cal Due: _____

h. Remove the antenna from the spacecraft using FAST-PROC-092 as a guideline. _____

i. Remove the antenna studs, nuts, and washers. Remove the cylinder from both rings. _____

60. Place the sliding contact onto jack receptacle

a. Take the sliding contact, part of the jack receptacle 2058-5305-00, and place it onto the exposed rod in the jack receptacle, through the top of the lower ring at the 0.066" connector pin hole. _____

70. Epoxy antenna cylinder (GD1524454) into mounting rings with Stycast 2850FT/Catalyst 9 (100:3.5)

a. Code 313.2 will provide the following epoxy: _____

1. Prepare an epoxy as follows: _____

Stycast 2850FT	100 pbw

Catalyst 9		3.5 pbw

b. With an #18 gauge needle on a syringe, apply a single bead of this epoxy throughout the 0.070" board slot in the lower ring. _____

c. Place the bottom of the antenna cylinder GD1524454 edge into the lower ring’s board slot. The cylinder should be rotationally aligned such that the 0.60" x 0.22" cutout is centered around the connector block and the final section of the sliding contact lies flat on the cylinder. (This will assure that the sliding contact is centered on the main input trace. _____

d. With an #18 gauge needle on a syringe, apply a single bead of the epoxy, prepared in step a, throughout the 0.070" board slot in the upper ring. _____

e. Place the upper ring onto the top of the antenna cylinder edge. The ring should be rotationally aligned such that two holes in each ring for the antenna studs are collinear. Placing the two antenna studs initially through the upper ring may help to obtain the alignment. _____

80. Insert the two antenna studs with nuts onto the mounting rings

a. Insert both studs into the lower ring, through to the upper ring. _____

b. Place a MS35649-264 nut onto each stud’s thread — do not tighten. _____

90. Integrate the assembly to the spacecraft Axial Boom

a. Install the antenna to the spacecraft per FAST-PROC-092. _____

100. Torque the two antenna studs to 15 in-lbs, allow the epoxy to dry for 48 hours

a. Torque both antenna studs to 15 in-lbs. The axial boom mating ring at the lower mounting ring should not warp during this operation. _____     _____ (QA)

Torque Wrench ID:  _____	Cal Due: _____

b. Thread another MS35649-264 nut on the antenna studs and torque against the lower nut to 15 in-lbs. The interface to the axial boom mating rings should now be flush. _____     _____ (QA)

Torque Wrench ID:  _____	Cal Due: _____

c.  Allow the assembly to dry at room temperature for 48 hours before handling. _____

d. A complete cure will take 7 days at room temperature. This should be achieved before Strength Verification is performed on the antenna. _____

110. De-integrate from the Axial Boom

a. After the 48 hours handling time, remove the antenna from the spacecraft using FAST-PROC-092 as a guideline. _____

120. Apply the two ITO Kapton pieces with transfer adhesive to antenna cylinder

a. Cut the upper ITO Kapton piece to measure 18.50"x1.00". _____

b. Cut the lower ITO Kapton piece to measure 17.75"x1.25". An additional 0.03" should be removed in width for about 1/8" in length at each end of the piece to accommodate the raised step at the connector location. _____

c. Apply Y966 transfer adhesive to each piece per FAST-PROC-042 steps 3 f-l. _____

d. Apply both pieces to the antenna cylinder per Code 724.1 approved document, GSFC Procedure for Application and Maintenance of Kapton tape, Aluminized Kapton tape, and ITO coated Kapton. The upper piece should be placed with one length edge at the upper ring/cylinder interface with its edges overlapping. The lower piece should be placed with the modified (0.03" slice) length edge at the lower ring/cylinder interface with its width edges an equal distance (approximately 1/8") from the main input trace. _____

130. Match drill two 0.113" holes through the lower mounting ring shelf and cylinder

a. Using a drill with a 90° attachment, match drill two 0.113" clearance holes through the ring shelf and the cylinder at the two 0.062" pilot holes. _____

b. Remove any burrs from the ring and cylinder. _____

140. Tighten the NAS1352N04-6 bolts, MS21043-04 nuts, MS15795-803 washers, and B0250-009-S belleville washers through the cylinder/shelf holes to compress 1/2

a. Place two B0250-009-S belleville washers in series on one NAS1352N04-6 bolt and insert it through the 0.113" clearance hole in the cylinder, exiting from the lower ring shelf. _____

b. Place an MS15795-803 washer and an MS21043-04 locknut on the exposed threads. Tighten the bolt to compress the belleville washers by approximately 1/2 of its relaxed height. _____     _____ (QA)

c. Repeat steps a and b for the other 0.113" mounting hole.

150. Solder the sliding contact to the main input trace

This event uses NHB 5300.4 (3A-2) as a reference document.

a. Verify that the final section of the sliding contact is lying flat on the cylinder. _____

b. Solder the sliding contact to the main input trace using standard 60 Sn/40 Pb solder. _____

160. Solder z-wires through the four ground holes on the cylinder per Procedure 12 Student Workbook for NHB5300.4 (3A-2)

a. Using #22 bus wire, solder (60 Sn/40 Pb) a z-wire through each of the four 0.031" ground holes in the cylinder per Procedure 12 of the Student Workbook for NHB 5300.4 (3A-2).  All wires should point in the circumferential direction. _____

170. Measure the antenna’s input VSWR

a. Calibrate the Wiltron Network Analyzer to measure VSWR using a reflection only, normal calibration from 2.0 to 2.3 GHz. _____

Network Analyzer ID:  _____	Cal Due: _____

b. Set the graph to display VSWR from 1.0 to 33.0 units. _____

c. Connect the test port 1 cable to the connector saver on the antenna input jack receptacle using a torque wrench calibrated to 8 in-lbs. _____          _____ (QA)

Torque Wrench ID:  _____	Cal Due: _____

d. Measure the data and plot the resulting graph. _____

e. Disconnect the antenna from the cable. _____

180. Epoxy the ITO Kapton to the adjacent mounting ring with Epon 828/ Versamid 140 (50:50) with Silflake 135 (20:80), allow to dry 48 hours

a. Code 313.2 will provide the following conductive epoxy: _____

1. Prepare an epoxy as follows: _____

Epon 828		50 pbw

Versamid 140	50 pbw

2. Mix this epoxy as follows to form a conductive epoxy: _____

Epoxy in step a.	20 pbw

Silflake 135		80 pbw

b. With a metal spatula, apply a spot of this epoxy, bridging the outer surface of the upper ITO Kapton piece to the upper ring. Any contact is acceptable to provide this grounding. _____

c. With a metal spatula, apply a spot of this epoxy, bridging the outer surface of the lower ITO Kapton piece to the lower ring. Any contact is acceptable to provide this grounding. _____

190. Epoxy across back of lower mounting ring shelf to cylinder ground plane with Epon 828/Versamid 140 (50:50) with Silflake 135 (20:80)

a. With a metal spatula, apply the epoxy prepared in Event 180 to the inside of the lower ring, over the shelf and the immediate surrounding area of the inside surface of the cylinder. Any contact is acceptable to provide this grounding, which is in addition to the mechanical contact performed in Event 140. _____

b. Allow the assembly to dry at room temperature for 48 hours before handling. _____

c. A complete cure will take 7 days at room temperature. This should be achieved before Strength Verification is performed on the antenna. _____

200. Seal the areas with conductive epoxy with a brush coating of Epon 828/Versamid 140 (50:50)

a. Code 313.2 will provide the following epoxy: _____

1. Prepare an epoxy as follows: _____

Epon 828		50 pbw

Versamid 140	50 pbw

b. Brush a thin coat (3-5 mils) of this epoxy over both areas epoxied in Event 180 and 190 which will seal these areas, preventing the conductive epoxy from flaking off and posing a contamination problem. _____

c. Allow the assembly to dry at room temperature for 48 hours before handling. _____

d. A complete cure of all epoxies applied will take 7 days at room temperature. This should be achieved before Strength Verification is performed on the antenna. _____

210. Receive ground planes and spacers from vendor

a. These parts are covered by separate certification logs developed by the vendor, who is responsible for delivering the parts. _____

220. Paint ground planes and spacers

All painting operations during this event are per a Code 724.1 approved procedure, GSFC Procedure for the Formulation/Application of a Family of Silicate Based Electrically Conductive Thermal Control Coatings.

a. Mask the two #6 threaded holes (with the helicoils) of the upper spacer (GC1524455). _____

b. Mask the #6 threaded hole (with the helicoil) and the #6 threads of the lower spacer (GC1524456). _____

c. Paint the six upper spacers with NS53B green paint. _____

d. Paint the six lower spacers with NS53B green paint. _____

e. Paint the upper ground plane (GD1524453) fully with NS53B green paint. _____

f. Paint the lower ground plane (GD1524459) fully with NS53B green paint. _____

g. Allow all parts to dry at room temperature for 24 hours. _____

230. Assemble ground planes to antenna with spacers and mounting hardware by torquing all NAS1352N06-6 bolts to 15 in-lbs

a. Connect one lower spacer to an upper spacer through one of the holes in the lower ground plane, by hand to a snug fit. Assured captivation is achieved

with the two bolts through the outer surface of the upper ground plane and the lower surface of the lower ring. _____

b. Repeat step a for the second set of spacers. The upper/lower spacer relationship should remain consistent with each set. _____

c. Repeat step a for the third set of spacers. The upper/lower spacer relationship should remain consistent with each set. _____

d. Repeat step a for the fourth set of spacers. The upper/lower spacer relationship should remain consistent with each set. _____

e. Repeat step a for the fifth set of spacers. The upper/lower spacer relationship should remain consistent with each set. _____

f. Repeat step a for the sixth set of spacers. The upper/lower spacer relationship should remain consistent with each set. _____

g. Place the assembly over the antenna such that the lower spacer meets the lower ring. _____

h. Bolt the assembly to the lower ring with six NAS1352N06-6 bolts by torquing to 15 in-lbs. _____     _____ (QA)

i. Place the upper ground plane over the antenna so the holes align with the upper spacers. _____

j. Bolt the upper ground plane to the upper ring with six NAS1352N06-6 bolts by torquing to 15 in-lbs. _____     _____ (QA)

240. Verify electrostatic cleanliness

a. Measure the resistance from the lower mounting ring to the following points to verify a resistance of <100 MΩ:

1. each of 6 lower spacers _____

2. lower ground plane _____

3. each of 6 upper spacers _____

4. upper ground plane _____

5. upper mounting ring _____

6. lower ITO Kapton piece _____

7. upper ITO Kapton piece _____

Meter ID:  _____		Cal Due: _____

250. Measure the antenna’s input VSWR and determine proper ground plane configurations, using radiation patterns w/mockup as criteria

a. Repeat Event 170 to measure the antenna’s input VSWR. _____

Measure the Radiation Patterns as follows:

Caution: Whenever personnel are inside the anechoic chamber, the transmit power should be reduced by 60 dB with the attenuators.

b. Temporarily mount the antenna to the mockup’s boom with six NAS1352N04-6 bolts, not torqued, just snug. _____

c. Set the transmitter and receiver to 2.215 GHz. _____

Transmitter ID:  _____	Cal Due: _____

d. Mount a linearly polarized Standard Gain Horn, model 12-1.7, at the transmit and receive sites for horizontal polarization, and connect the cables to their input ports. _____

e. Command the positioner to Azimuth=0°, Head=0°, Elevation=0°. _____

f. Adjust the signal levels to achieve a reference signal of 0 ± 2 dB and a receive signal between -10 and 0 dB. _____

Receiver ID:  _____	Cal Due: _____

g. Preset the receive signal to a value of 6.25, per the Standard Gain Horn reference curve. Record on the chart that this forces -10 dB to be the ‘0 dBi’ line. _____

h. Zero the transmit power meter to 0 dB, relative mode. _____

Power Meter ID:  _____	Cal Due: _____

i. Determine the measurement tolerances by recording the received signal for applied transmit powers of 0, -10, -20, and -30 dB below nominal. _____

j. Remove the Standard Gain Horn from the receive site. _____

k. Mount the mockup with the antenna, and connect the cable to the connector saver on the antenna input jack receptacle using a torque wrench calibrated to 8 in-lbs. _____     _____ (QA)

Torque Wrench ID:  _____	Cal Due: _____

l. Setup the positioner program as follows: _____

Record Mode	Scan Axis: A	Scan Start: -175

Scan Stop: +175	Scan Dir 1: FWD	Scan Speed: 350

Scan Incr: 1		No of Scans: 36	Scan Dir 2: RET

Step Axis: C		Step Dir: FWD	Step Incr: 5

m. Scroll to a new chart and run the positioner program. _____

n. Disconnect the cable to the antenna input port and remove the mockup from the positioner. _____

It is expected that the initial ground plane designs may be unsatisfactory. If so, an EO will be written to modify the ground planes and re-run steps k-n, or if the equipment has been turned off and on, re-run steps b-n for calibration and test, to obtain an acceptable transmit pattern and then continue with the procedure.

o. Set the transmitter and receiver to 2.03965 GHz. _____

Repeat the steps d-n to obtain the receive radiation pattern. _____

260. Weigh Antenna

a. Zero the scale. _____

Scale ID:  _____		Cal Due: _____

b. Place the antenna on the scale and record the weight. _____

270. Strength Verification per FAST-TEV-053

a. Perform referenced procedure. _____

280. Re-measure the antenna’s input VSWR and radiation pattern on the mockup

a. Repeat Event 250. _____

290. Thermal Verification per FAST-TEV-054

a. Perform referenced procedure. _____

300. Re-measure the antenna’s input VSWR and radiation pattern on the mockup

a. Repeat Event 250. _____

310. Delivery to I&T

a. Deliver the antenna to the spacecraft for mechanical and electrical integration.